## Slide 1: Next-generation Latent Fingermark Detection Using Functionalised Silicon Oxide Nanoparticles
Timothy Lee
PhD Candidate
Western Sydney University, School of Science and Health
Prof. Chris Lennard 1
Prof. Claude Roux 2
Dr Sébastien Moret 2
Dr Fehmida Kanodarwala 2
Dr Xanthe Spindler 2
Dr Val Spikmans 1
ANZFSS NSW Branch Meeting – 10 October 2018
1 Western Sydney University, School of Science and Health
2 University of Technology Sydney, Centre for Forensic Science

## Slide 2: Why Silicon Oxide Nanoparticles?
Increasing research interest for latent fingermark detection in the past decade
Small size
  Average diameter of around 70 – 80 nm (via reversed micro-emulsion synthesis)[1,2]
Versatile modifiable surface
  External layer of silanol (Si-OH) and siloxane (Si-O-Si) groups[3]
Extended optical properties
  Potential of using a variety of dye molecules in their inner structure[1]
1. Moret, S., Bécue, A. & Champod, C. 2014, Nanotechnology, vol. 25, no. 42, p. 425502.
2. Moret, S., Bécue, A. & Champod, C. 2016, Forensic Science International, vol. 259, pp. 10-8.
3. Bécue, A. & Cantú, A. 2012, Lee and Gaensslen's Advances in Fingerprint Technology, Third Edition, CRC Press, pp. 307-80.

## Slide 3: Previous Research
An insight into the use of silicon oxide nanoparticles (SiO2 NPs) for latent fingermark detection was published in 2016[2]
A RuBpy-doped CES-functionalised SiO2 NP reagent was proposed
A set of detection parameters was suggested for application
  A working formulation with the use of the functionalised NPs to detect latent fingermarks
2. Moret, S., Bécue, A. & Champod, C. 2016, Forensic Science International, vol. 259, pp. 10-8.

## Slide 4: Research Aims
Design and synthesise a novel SiO2-based NPs for improved fingermark detection
Optimise and validate the technique for latent fingermark detection
The novel and validated technique will be applicable in standard police laboratories as a user-friendly latent fingermark detection method
Make something new
Make it work
Make it better and actually usable
Research in a Nutshell – TL;DL Version

## Slide 5: Concentration of the Nanoparticles
The functionalised NPs are diluted by half in the working formulation[2]
  How much is actually enough to detect latent fingermarks?
  An optimum concentration
Different NP concentrations were compared against the published formulation[2]
  4x, 10x, 20x, 40x, 80x and 200x dilutions of the NPs
2. Moret, S., Bécue, A. & Champod, C. 2016, Forensic Science International, vol. 259, pp. 10-8.

## Slide 6: Concentration of the Nanoparticles
20x diluted
40x diluted
2x diluted
4x diluted
10x diluted
80x diluted
200x diluted
Transparent polypropylene

## Slide 7: Concentration of the Nanoparticles
Detection quality increased with higher dilutions
At higher concentrations there are inter-nanoparticle attractions
  These attractions hinder interactions with fingermark residues
A 40x dilution was employed for the working formulation as a modification

## Slide 8: Treatment Temperature and Immersion Time
The functionalised NPs are suggested to chemically interact with the fingermark secretions[1]
Hypothesis: detection rate and detection effectiveness will increase at higher temperature, hence a shorter immersion time
Comparison experiments performed at 3°C, 23°C (room temperature) and 45°C
1. Moret, S., Bécue, A. & Champod, C. 2014, Nanotechnology, vol. 25, no. 42, p. 425502.

## Slide 9: Treatment at Various Temperature Points
23°C
3°C
23°C
45°C
3°C
45°C

## Slide 10: Treatment Temperature and Immersion Time
Detection effectiveness improved at higher temperature points
A possible shorter immersion time than one hour?
Comparison experiments performed at room temperature for one hour and 45°C with shorter immersion times

## Slide 11: Shorter Immersion Times at Higher Temperature
PAGE 10
1 hour (23°C)
15 min (45°C)
1 hour (23°C)
5 min (45°C)
15 min (45°C)
5 min (45°C)

## Slide 12: Optimised Treatment Temperature and Immersion Time
Treatment temperature points
  30°C vs 35°C vs 40°C (reduction from 45°C)
Immersion time
  2 min vs 3 min vs 5 min
Treatment at 40°C for 5 min was incorporated as a modification

## Slide 13: Detection Parameters
Published
SiO2 NPs (2x diluted)
Room temperature
1 hour
Modified
H2O
5 mins
H2O
5 – 10 mins
SiO2 NPs (40x diluted)
35°C – 40°C
3 – 5 mins
H2O
5 mins
H2O
5 – 10 mins

## Slide 14: Comparison of the Two Detection Parameters
Natural fingermark specimens
  3 donors (strong, average and weak)
  3 substrates (aluminium foil, transparent PP and green PE)
  2 age intervals (10 days and 3 months)
  4 fingers with 4 depletions
288 fingermark specimens were processed and evaluated
A comparative scoring system was used for fingermark assessment
  Based on the University of Canberra (UC) scale

## Slide 15: Overall Performance

## Slide 16: Take-home Messages
Modification and optimisation of the published detection parameters
  A shorter immersion time (5 min) at a higher temperature (40°C) during fingermark treatment can significantly improve detection quality
  Comparison study showed that the modified detection parameters gave superior results
A manuscript of the research findings has been submitted for publication
My parents still think that I am doing a DNA project…

## Slide 17: Acknowledgements
Australian Research Council
  Linkage Project (LP160100351)
Rofin Australia Pty Ltd
Australian Federal Police
Victoria Police
ANZFSS NSW Branch Award

## Slide 18
Questions
Timothy Lee
timothy.lee@westernsydney.edu.au