## Slide 1: Next-generation Latent Fingermark Detection Using Functionalised Silicon Oxide Nanoparticles
Timothy Lee
PhD Candidate
Western Sydney University, School of Science and Health
Prof. Chris Lennard 1
Prof. Claude Roux 2
Dr Fehmida Kanodarwala 2
Dr Sébastien Moret 2
Dr Xanthe Spindler 2
Dr Val Spikmans 1
2019 3rd International Conference on Materials Sciences and Nanomaterials – 23 July 2019
1 Western Sydney University, School of Science and Health
2 University of Technology Sydney, Centre for Forensic Science

## Slide 2: Fingermark Evidence in Forensic Science
Early days of dactyloscopy (fingerprinting)
  Pioneer studies dated back to the end of the 19th century[1]
  Argentina became the first country to formally file criminal records solely using fingerprints in 1896[2]
  It has since been the foundation of forensic identification for more than a century
The gold standard of forensic identification in criminal investigations
  The ”never-change-in-a-lifetime” feature of human fingerprints
  SUPERIOR (able to differentiate identical twins, unlike DNA) discriminating power
1. Aaron, J.U. 2010, Forensic Dentistry, Second Edition, CRC Press, pp. 79-102.
2. Vivianne, G. & Dave, C. 2006, Forensic Human Identification, CRC Press, pp. 56-72.

## Slide 3: The Human Fingerprints
Three levels of friction ridge skin features[3]
  Level 1 – basic general patterns
3. Champod, C., Lennard, C., Margot, P. & Stoilovic, M. 2016, Fingerprints and Other Ridge Skin Impressions, CRC Press, pp. 37-38.
  Level 3 – pores
  Level 2 – minutiae
  Ridge ending
  Bifurcation
  Dot

## Slide 4: Latent Fingermarks
Chemical constituents of the human fingermarks
  Sources – Eccrine (aqueous secretions) and sebaceous glands (lipid secretions)
  Latent fingermark residues are therefore a combination of water and non-water soluble components
  Amino acids and lipids are two major groups of constituents of latent fingermark residues
Video: TIMELAPSE VISION. 2016, Fingerprints and sweat glands, Available at: https://www.youtube.com/watch?v=lOaFeGreAJw.

## Slide 5: Latent Fingermark Detection and Enhancement
Various conventional techniques
  Powder dusting
  Amino acid reagents (e.g. 1,2-indanedione-zinc and ninhydrin)
  Cyanoacrylate (CA) fuming + luminescent dye staining
  Metal deposition
Major drawbacks of conventional techniques
  Inabilities to develop fingermarks on substrates with complex background chemistries
  Struggle to detect some fingermarks that are present[4]
Need of new techniques
4. Chadwick, S., Moret, S., Jayashanka, N., Lennard, C., Spindler, X. & Roux, C. 2018, Forensic Science International, vol. 289, pp. 381-9.

## Slide 6: Silicon Oxide Nanoparticles
5. Bécue, A. & Cantú, A. 2012, Lee and Gaensslen's Advances in Fingerprint Technology, Third Edition, CRC Press, pp. 307-80.
6. Moret, S., Bécue, A. & Champod, C. 2014, Nanotechnology, vol. 25, no. 42, p. 425502.
7. Moret, S., Bécue, A. & Champod, C. 2016, Forensic Science International, vol. 259, pp. 10-8.
Versatile modifiable surface[5]
+ extended optical properties[6]
+ small size[6,7]

## Slide 7: How Does It Work?
Visualisation
Synthesis
RuBpy-doped (core)
CES (carboxyethylsilanetriol)-functionalised SiO2 NPs
48 hours
Application
Rinse
H2O
Rinse
H2O
Colloidal dispersion
RuBpy-CES-SiO2 NPs
450 nm
excitation
590 nm
emission

## Slide 8: Luminescent Fingermarks
An example of a latent fingermark detected and enhanced with RuBpy-doped CES-SiO2 NPs
Visualised in luminescence mode with 450 nm excitation and observation at 590 nm

## Slide 9: Modification and Optimisation of Detection Parameters
Insights from a previous study[7]
  Promising new latent fingermark detection technique
  Optimisation of detection parameters required
Modification and optimisation of the previous detection parameters
  Lower concentration of NPs used in the working colloidal dispersion
  Higher treatment temperature with shorter immersion time
  Comparison study showed that the modified detection parameters gave superior results[8]
7. Moret, S., Bécue, A. & Champod, C. 2016, Forensic Science International, vol. 259, pp. 10-8.
8. Lee, P.L.T., Kanodarwala, F.K., Lennard, C., Spindler, X., Spikmans, V., Roux, C. & Moret, S. 2019, Forensic Science International, vol. 298, pp. 372-83.

## Slide 10: Modified Detection Parameters
Colloidal dispersion
40x dilution of the NPs
40 °C on a hot plate
5 min immersion
Colloidal dispersion
2x dilution of the NPs
Room temperature
1 hour immersion
Previous
Modified
Rinse
H2O
5 min
Rinse
H2O
5 – 10 min
Rinse
H2O
5 min
Rinse
H2O
5 – 10 min

## Slide 11: Results
Aluminium foil
Previous
Modified
Previous
Modified
Transparent polypropylene
Green polyethylene
Previous
Modified

## Slide 12: Refinement of the Surface Functionalisation
Different concentrations of CES used in synthesis for surface functionalisation
  –COOH, carboxyl functionalisation
  NPs synthesised with lower concentrations showed improvements on detection quality
Comparisons of 100%, 80%, 60% and 50% of CES
  50 – 60% of CES (of the original amount) is suggested to be the optimum concentration
  Lowering the amount of CES used increases detection quality
  With the original amount of CES used (100%), the SiO2 NP surface is “over-occupied” by CES molecules
  This negatively impacts the degree of effective interactions between CES molecules and fingermark residues

## Slide 13: Simplified Application
Treatment using a shaking incubator to replace hot plate for improved practicality

## Slide 14: Latest Detection Parameters
Shaking incubator is a practical alternative to hot plate treatment
  Comparison with hot plate treatment showed no difference in detection quality
  More steady temperature control
  Capacity to treat larger and more items simultaneously
50% CES-SiO2 with shaking incubator treatment
  Improved “sensitivity” of the processed fingermark specimens from using 50% CES-SiO2 NPs with shaking incubator than 100% CES-SiO2 NPs with hot plate treatment

## Slide 15: Comparison with a Conventional Method
Comparison of the SiO2 NPs (with the latest detection parameters) with a benchmark technique – cyanoacrylate fuming (CAF) + rhodamine 6G (R6G) staining
4 Fingers
4 depletions
6 Donors
3 males
3 females
3 Ages
1 | 3 | 6 months
6 Substrates
Al foil | PP | PE
glass | paint | tile
CAF + R6G
SiO2 NPs
3456 fingermarks

## Slide 16: Cyanoacrylate Fuming + Luminescent Dye Staining
Cyanoacrylate (CA) fuming[3]
  CA liquids are colourless polyesters that interact with latent fingermark residues and form hard, white polymers over ridges
  Commercially available and widely accepted since late 1970s for latent fingermark development on non-porous surfaces
Luminescent dye staining for CA fumed fingermarks[3]
  Immersion of CA treated fingermarks into a luminescent dye solution for application
  Rhodamine 6G (R6G) has a high luminescence efficiency and is commonly used
3. Champod, C., Lennard, C., Margot, P. & Stoilovic, M. 2016, Fingerprints and Other Ridge Skin Impressions, CRC Press, pp. 37-38.
CAF + R6G developed fingermark
Visualisation:
530 nm excitation
590 nm emission

## Slide 17: Results – 1-month-old Fingermarks
Aluminium foil
Green polyethylene
RuBpy-CES-SiO2 NPs
450 nm; 590 nm
CAF + R6G
530 nm; 590 nm
RuBpy-CES-SiO2 NPs
450 nm; 590 nm
CAF + R6G
530 nm; 590 nm
RuBpy-CES-SiO2 NPs
450 nm; 590 nm
CAF + R6G
530 nm; 590 nm
Aluminium foil

## Slide 18: Conclusions
RuBpy doped CES-functionalised SiO2 NPs for latent fingermark development has been modified and optimised
Preliminary comparison results with CAF + R6G (a benchmark technique) show that
  CAF + R6G is more donor-dependent
  SiO2 NPs method is more substrate-dependent
Work to utilise upconverting nanoparticles (UCNPs) with SiO2 shell is underway within our research group

## Slide 19: Questions for the audience
Some research hurdles so far
Not applicable on glass surface
Background staining problem on aluminium foil
Difficulties to synthesise UCNPs@SiO2 shell

## Slide 20: Acknowledgements
Australian Research Council
  Linkage Project (LP160100351)
Rofin Australia Pty Ltd
Australian Federal Police
Victoria Police
WSU-UTS Fingerprint Research Group

## Slide 21
www.iafs2020.com.au
iafs2020@arinex.com.au
iafs2020
21-25 September 2020
Sydney, Australia

## Slide 22
Questions
Timothy Lee
timothy.lee@westernsydney.edu.au